## Slide 1: N, N-dimethyldodecylamine (DDA) Quantification
2024/08/19
Danica Levesque
CASST 2024

## Slide 2: SNO+
  Located in Creighton mine, 6800 ft underground
  Multipurpose particle astrophysics detector, focuses on the search for neutrinoless double beta-decay
  12 m diameter acrylic vessel filled with 780 tons of liquid scintillator, linear alkylbenzene (LAB)
Notes: Extra slide that talks about scintillator

## Slide 3: The Scintillator Cocktail
Linear Alkylbenzene (LAB)
2, 5-Diphenyl Oxazole
..
N, N-dimethyldodecylamine (DDA)
Scintillator
Aromatics  delocalized electrons are easily excited
1,4-bis[2-(2-methylphenyl)ethenyl]-benzene
Wavelength Shifters
Conjugation  decreases energy transition, increasing the emitted wavelength
Stabilizer
Amine  electron donors help stabilize free radical and prevent oxidative reactions

## Slide 4: DDA Purification
DDA will be distilled three separate times to obtain different levels of purity
The distillation plant will be washed with LAB in between batches

## Slide 5: LAB and DDA UV-Vis Spectrum
At the isosbestic point, both LAB and DDA have the same absorptivity
Helps discriminate the absorption contributions of LAB/DDA at those wavelengths
Expected to be a linear function
Absorbance (AU)
Wavelength (nm)
200
250
300
350
400
450
0
0.5
1
1.5
2
2.5
3
3.5
4

## Slide 6: Procedure
DDA
LAB

## Slide 7: Concentration Curve With UV-Vis

## Slide 8: Concentration Curve With UV-Vis – Trial 2

## Slide 9: Concentration Curve With UV-Vis – Trial 1 and 2
Shift was due to minor changes in the LAB spectrum at the isosbestic point.
This change can be corrected with previous data of LAB.

## Slide 10: Concentration Curve With UV-Vis –Trial 3
Absorbance (AU)
Wavelength (nm)
The lack of the fit is attributable to DDA shifting, maybe due to improper storage (N2).

## Slide 11: Problems with UV-Vis
Limited by the isosbestic point for the analysis
Light sensitivity and oxygen sensitivity
  This would require constant correction and a lot of work to understand this behaviour

## Slide 12: Concentration Curve With Density

## Slide 13: Concentration Curve With Density

## Slide 14: Summary
  Light and oxygen influences the spectroscopic properties of LAB and DDA
  Concentration curve with UV-Vis data is not repeatable
  Plotting the weight of the sample versus the concentration of DDA utilizes the differences in density of the two compounds
    Need to control temperature and humidity
    Results were repeatable!

## Slide 15
Questions?