## Slide 1: Transfer Station & Scintillator Plant Upgrade for SNO+
2025/04/17
William Zhang
Co-op Winter 2025

## Slide 2: SNO+ Overview
Main physics goal: observe 0vbb through scintillation
Scintillator = LAB organic(oil)
THEY DON’T MIX
TeA + BD  TeBD
TeBD/DDA mixture cycle into detector
Source = TeA aqueous(water)

## Slide 3: BD/DDA Transfer Station
Want Te-source in detector  DDA & BD into plants UG to mix with TeA
DDA:
distilled on surface
shipped UG in drums
Goal of Transfer Station:
drum to TeDiol Plant for mixing
  Then load into detector via Scint
BD:
shipped UG in drums
Goal of Transfer Station:
drum to Scint Plant for distillation
  Then to TeDiol for rxn/mixing
  Then load into detector via Scint

## Slide 4: BD/DDA Transfer Station – What do we need?
Drum  Pump  Pipe
  Hand valves to direct flow
  Flowmeter to monitor flow
N2 cover gas
  Manometer to monitor pressure
  Safety valve & break valve for extreme pressure
Compressed air to power pump
  Pressure regulators & solenoid valves to control flow
Support Structures (Unistruts & Aluminum Panels)

## Slide 5
The unistrut The panel The hand valves
DDA Transfer Station

## Slide 6
The Dewar
NITROGEN
THE DEWAR

## Slide 7

The
Unistrut

The Panel
BD Transfer Station

## Slide 8
The hand valves The backside

BD Transfer Station The pump

## Slide 9
Manometer

## Slide 10
BD
Transfer
Station

## Slide 11: BD/DDA Transfer Station – Current Status
Near complete
When complete, have capability to transfer BD/DDA into plant

## Slide 12: Compatibility: Carbon black-filled PFA hose with LAB/BD
Why:
confirm material doesn’t change optical properties of experiment
What:
Carbon black-filled PFA hose
    connect BD drum to Scint Plant
Procedure:
Fill hose with LAB/BD
Take 4 samples: day 0 (control), day 1, day 7, day 14
Compare UV-Vis

## Slide 13
Setup

## Slide 14
Result
They are compatible
Brought UG & connected week of Apr 14
LAB
BD

## Slide 15: Scint Plant Upgrade
The column is leaking
install N2 supply + gauges at flanges to monitor leak
PIPE
MANIFOLD
GAUGE

## Slide 16

The gauge

The manifold

The pipe

## Slide 17

The gauge

More gauge

The manifold

## Slide 18
The manifold

The gauge
