## Slide 1: Radon Mitigation, Removal, and Testing at SNO+
Julia Gorovitz
Supervisors – Dr. Christine Kraus, Dr. Nasim Fatemighomi, Juliette Deloye
CASST 2025
1

## Slide 2: Table of contents 01. 04. 02. 05. 03.
SNO+ Overview
Why is radon such a problem?
Zeolite trap system overview
Introduction
Radon Assays
Zeolite Traps
Results and Future Directions
Acknowledgements and References
2

## Slide 3: Introduction 01.
SNO+ Overview
3

## Slide 4: The SNO+ experiment Overview Goals
Cavity with 7400 tones of UPW
PSUP – Support structure with 9300 PMTs
Acrylic vessel (AV)
2 km rock overburden
Shielding from cosmic radiation
Neutrinoless double beta decay (0νββ)
Solar neutrinos
Geo antineutrinos
Reactor antineutrinos
Supernova neutrinos
4
BNL | Chemistry | Neutrino and Nuclear Chemistry | Collaborations. Bnl.gov. https://www.bnl.gov/chemistry/nnc/collaborations.php (accessed 2025-08-09).
The SNO+ Experiment. Journal of Instrumentation 2021, 16 (08), P08059–P08059. https://doi.org/10.1088/1748-0221/16/08/p08059.
‌

## Slide 5: The SNO+ experiment Radon mitigation techniques
High-purity Nitrogen Cover Gas with constant monitoring – 3000L!
 1.9 × 10−4 reduction relative to mine air
Nitrogen Purging and Overpressure
Radon Trap in Nitrogen Line
UPW Purification Systems
Radon assays
5
2) The SNO+ Experiment. Journal of Instrumentation 2021, 16 (08), P08059–P08059. https://doi.org/10.1088/1748-0221/16/08/p08059.
‌

## Slide 6: Radon Assays 02.
Why is radon a problem in the SNO+ detector?
6

## Slide 7: The Uranium-238 decay chain
Radon-222 isotope
Inert gas
Short half-life (3.82 days)
Three subsequent α-decays
Bismuth-214
Very short half-life (19.7 minutes)
BiPo β-decay can generate energy in the ROI for 130Te 0νββ (red in the plot)
Lead-210
Very long half-life
Deposits in the experiment
7
(MeV)
(Arbitrary Units) – log scale
Sangam@hri, W. Neutrinoless Double Beta Decay. https://indico.cern.ch/event/218049/contributions/1519262/attachments/351513/489797/Warner_26th.pdf
Fang, F. Radon Plate-out and the Effects of Airflow and Electric Charge for Dark Matter Experiments. 2024, 8 (1, 2024). https://doi.org/10.25172/jour.8.1.1.
‌
‌

## Slide 8: Radon Assays in SNO+ Gas Assays
8

## Slide 9
*Charcoal trap attached
Sample path to Lucas Cell in purple
Radon Assays in SNO+ Gas Assays
9
5) Hussain, A. Evaluating 238U external background for SNO+ experiment using radon Aasays and 214Bi analysis. Scholaris.ca. https://laurentian.scholaris.ca/items/1c991a03-7714-41fe-9080-59a11f9716e4 (accessed 2025-08-09).
‌

## Slide 10: Zeolites 03.
Zeolite trap system overview
10

## Slide 11: Zeolites
Zeolites are porous aluminosilicates
     SiO₄ / AlO₄ tetrahedra
    Why use it in assays/ as a radon trap?
  High Adsorption Efficiency
Selective Trapping
Temperature Control
Re-generability
11
Effect of Surface Modification of Natural Zeolite on Ammonium Ion Removal from Water Using Batch Study: An Overview. Water, Air, & Soil Pollution 2022, 233 (11). https://doi.org/10.1007/s11270-022-05948-4.
What is Zeolite?_Chemicalbook. Chemicalbook.com. https://www.chemicalbook.com/Article/What-is-Zeolite.htm (accessed 2025-08-09).
‌
‌

## Slide 12: Motivation and Studies - Zeolites
 Ag-ETS-10
High absorption capacity at room temperature
All other traps need cryogenic cooling
Higher trapping capacity
Radon filter for the nitrogen cover bags
   Types of assays done to better understand the zeolite
Emanation at different temperatures
Calibration
Background
12

## Slide 13: Results and Future Directions 04.
13

## Slide 14: Zeolite – main assay results
Date | Assay type | Result (atoms/day)
May 27, 2025 | Emanation (150°C) | 2719.9
June 18, 2025 | Emanation (150°C) | 434.89
June 27, 2025 | Emanation (at room temp) | 34.51
July 31, 2025 | Calibration* (at 150°C) | 49.8
August 1, 2025 | Background (300°C) | 689.21
Emanation assay results:
At 150°C, 20h baking showed an improvement of 84% less atoms/day
Low counts for the calibration assay  high counts for the next day background
At calibration, comparing to 16000 atoms/day in calibration can
14

## Slide 15: Next Steps for SNO+
Calibration assay done entirely at 300°C
   Accurately analyze trapping capacity
  Re-do a background assay
   Without the interference seen from the assay . done the day before
  Continue baking/ purging the zeolite to see how low the emanation/ background gets
   Explore the possibility of using the zeolite for
  assays
15

## Slide 16: Summary
Radon Problem – Rn-222 from U-238 decay chain produces backgrounds in the ROI through several α and β-decays
Mitigation Methods – Nitrogen cover gas, purging/overpressure, radon traps, and UPW purification
Radon Assays – Used the SNO+ gas assay board to analyze a new type of radon trap
Zeolite Choice – Silver-exchanged ETS-10 for high adsorption efficiency, noble gas selectivity, no need for cryogenic cooling
Assay Results – Baking at 150 °C reduced emanation by 84%; calibration and background assays show ambiguous results, need further examination
Next Steps – High-temp calibration at 300 °C, continued baking/purging to further reduce background, re-do background and emanation assays, evaluate trap for routine assays
16

## Slide 17: Aknowledgements 05.
17

## Slide 18: References
18
BNL | Chemistry | Neutrino and Nuclear Chemistry | Collaborations. Bnl.gov. https://www.bnl.gov/chemistry/nnc/collaborations.php (accessed 2025-08-09).
Albanese, V.; Alves, R.; Anderson, M. R.; Andringa, S.; Anselmo, L.; E. Arushanova; S. Asahi; Askins, M.; Auty, D. J.; Back, A.; Back, S.; F. Barão; Barnard, Z.; Barr, A. J.; Barros, N.; Bartlett, D. T.; Bayes, R.; Beaudoin, C.; Beier, E. W.; Berardi, G. The SNO+ Experiment. Journal of Instrumentation 2021, 16 (08), P08059–P08059. https://doi.org/10.1088/1748-0221/16/08/p08059.
Sangam@hri, W. Neutrinoless Double Beta Decay. https://indico.cern.ch/event/218049/contributions/1519262/attachments/351513/489797/Warner_26th.pdf
Fang, F. Radon Plate-out and the Effects of Airflow and Electric Charge for Dark Matter Experiments. 2024, 8 (1, 2024). https://doi.org/10.25172/jour.8.1.1.
Hussain, A. Evaluating 238U external background for SNO+ experiment using radon Aasays and 214Bi analysis. Scholaris.ca. https://laurentian.scholaris.ca/items/1c991a03-7714-41fe-9080-59a11f9716e4 (accessed 2025-08-09).
Yadav, V.; Rani, M.; Kumar, L.; Singh, N.; Ezhilselvi, V. Effect of Surface Modification of Natural Zeolite on Ammonium Ion Removal from Water Using Batch Study: An Overview. Water, Air, & Soil Pollution 2022, 233 (11). https://doi.org/10.1007/s11270-022-05948-4.
What is Zeolite?_Chemicalbook. Chemicalbook.com. https://www.chemicalbook.com/Article/What-is-Zeolite.htm (accessed 2025-08-09).
‌
‌
‌

## Slide 19: Special thanks to:
Dr. Christine Kraus
Dr. Nasim Fatemighomi
Juliette Deloye
Dr. Mark Ward
Adil Hussein
Peter Qin
Keegan Paleshi
Yusuf Ahmed
Dr. Aleksandra Bialek
Dr. Ryan Bayes
Matt Depatie
Noah Fenlon
Semoore Tijani
Emilio de la Cruz
Brianna Binoy
& All my other colleagues who made the semester unforgettable
19