## Slide 1: Developing Silver Doped Zinc Sulfide Scintillator for Lucas Cell 222Radon Counting
Kacper Rogut (He/Him)
Undergraduate Chemistry Assistant

## Slide 2: Background: Radon at SNOLAB

## Slide 3: Intro to the project
First thing to understand is Radon
  Noble Gas
  α-particle decay
  222Rn half-life ~4 days
Emanates from materials and from underground
A significant background source in low background experiments

## Slide 4: Intro to the project
SNOLAB experiments that use Rn measurements
  SNO+
  CUTE
  DAMIC
  DEAP-3600
  XLZD
- Radon assay boards used for​
  High sensitivity radon emanation measurement​

## Slide 5: Improving radon assay capabilities is a priority at SNOLAB

## Slide 6: Background
Your new favourite words: Lucas Cell and ZnS:Ag
Lucas Cell (LC)
ZnS:Ag

## Slide 7: Questions
- What is a Lucas Cell?
  Measures Radon decay using α-particle scintillator, ZnS:Ag
222Rn
α-particle
Light
--> 218Po
- Photomultiplier tube (PMT) collects and amplifies light so it can be analyzed​
- Who is Lucas?
Lucas Cell (LC)​
​

## Slide 8: Background- Scintillation
  ZnS scintillation requires an activator.
    Silver provides a bright blue light and is ideal for alpha
  Band gap is forbidden
  Excitation of electron
  Energy transfer to an activator (Ag)
  De-excites and emits photon
Valence Band
Excitation Band
Ag excitation band
Ag Ground state
α
Visible Light
UV Light

## Slide 9: Background
Should we buy commercial?
Lucas Cell (LC)
ZnS:Ag
LC is coated with ZnS:Ag​​
  Too much background for our low-background experiments!​​
  This is my role... synthesizing low-background ZnS:Ag​
NO

## Slide 10: Experiment - Synthesis
Zinc Acetate and Sodium sulfide as initial reagents​
Synthesize zinc sulfide
2. Silver doping

## Slide 11: Experiment - Synthesis
Zinc Sulfide is formed as a precipitate.
    Everything else stays in solution.​
  Product is filtered and collected as a wet solid​
=> Bulk ZnS​

## Slide 12: How do you remove background?

## Slide 13: Selective Precipitate

## Slide 14: Experiment - Selective Precipitate
  This method takes advantage of Ksp, product solubility
          Smaller Ksp = first to precipitate
  The impurities uranium, thorium, and lead have extremally small Ksp in this reaction​

## Slide 15: Experiment - Selective Precipitate
Zinc Acetate Solution
Sodium sulfide
Solid Waste
Precipitated Pb Impurities
Add a few drops
ZnS + unprecipitated impurities
95% mol equivalent
SP ZnS
Filter Precipitated ZnS
Liquid Waste
Filtrate​

## Slide 16: ZnS Background Testing

## Slide 17: Experiment - Radon Counting
Three samples we tested:
  In-house SP ZnS
  In-house bulk ZnS
  Commercial ZnS:Ag
Initial background testing:​

## Slide 18: Experiment - Radon Counting
    Acrylic windows, same material as LC
    Sandwich with a scintillating commercial ZnS:Ag
  Developed new procedure for Radon counting

## Slide 19: Experiment - Radon Counting
SP, Bulk, or Commercial ZnS
Commercial ZnS:Ag
ZnS Coating
Visible Light​

## Slide 20: Experiment - Window Radon Counting
Sandwich:
Commercial on commercial ZnS:Ag
~12 Radon counts/day
~6 Radon counts/day​

## Slide 21: Experiment - Window Radon Counting
Sandwich:
In-House ZnS on commercial ZnS:Ag​
~18 Radon counts/day
~3 Radon counts/day​

## Slide 22: Experiment - Window Radon Counting
  This demonstrates our new Rn assay system is working and lowering ZnS:Ag background
Bottom Window | Top Window | Radon Count / Day
In-house ZnS SP | Commercial Eljean | 3
Commercial St.G | Commercial St.G | 6
Commercial St.G | Commercial Eljean | 12
In-house ZnS Bulk | Commercial Eljean | 18
Two coatings, therefore SP may be as low as 0 counts / day

## Slide 23: Silver Doping

## Slide 24: Experiment - Silver Doping Oven
Silver is baked into the ZnS
Air causes oxidation
=> ZnO
Makeshift inert oven

## Slide 25: Experiment - Silver Doping Oven Set Up
Argon Tank
Oven
Charcoal Trap
Vacuum

## Slide 26: Experiment - Silver Doping Procedure
The sample mixture:
ZnS
Silver acetate
Salt (flux)
Elemental sulfur (O2 scavenger) ​
Synthesis of Silver-Activated Zinc Sulfide (Zns:Ag) Powder by Thermal Diffusion Method for Production of Thin Film Alpha Scintillators by Mehdi Sohrabi, Fereshteh Saheli and Kheirollah Mohammadi

## Slide 27: Experiment - Silver Doping Procedure
Create vacuum, fill with Ar x5
Bake moisture off at 120°C
Synthesis of Silver-Activated Zinc Sulfide (Zns:Ag) Powder by Thermal Diffusion Method for Production of Thin Film Alpha Scintillators by Mehdi Sohrabi, Fereshteh Saheli and Kheirollah Mohammadi

## Slide 28: Experiment - Silver Doping Procedure
3. Heat to 350°C
Sulfur melts
Displaces air in pores
4. Heat slowly to 950°C
Sulfur boils, reacts with O2 and leaves as gas
ZnS and Ag melts at 900°C ​
5. Cool to room temp
Wash with UPW to remove salt
Synthesis of Silver-Activated Zinc Sulfide (Zns:Ag) Powder by Thermal Diffusion Method for Production of Thin Film Alpha Scintillators by Mehdi Sohrabi, Fereshteh Saheli and Kheirollah Mohammadi

## Slide 29: Silver Doping Results

## Slide 30
Commercial Zns:Ag
In-House Zns:Ag

## Slide 31: Experiment - Silver Doping Results
Doping worked
There is light
    Green / Blue

## Slide 32
https://www.gigahertz-optik.com/en-us/service-and-support/knowledge-base/basics-light-measurement/light-color/
Thank you to
Prof. Stefan Siemann
School of Natural Sciences Laurentian University
*Amplitudes are normalized

## Slide 33
https://www.gigahertz-optik.com/en-us/service-and-support/knowledge-base/basics-light-measurement/light-color/
Thank you to
Prof. Stefan Siemann
School of Natural Sciences Laurentian University
Light
Light
PMT

## Slide 34
In-House Zns:Ag
Old In-House Zns:Ag
Commercial Zns:Ag

## Slide 35: What Went Wrong?
Too much silver
    Measured ~1500ppm compared to ~600ppm Ag
    This quenches light efficiency
Paper's procedure found ~80% efficiency compared to commercial ​
OR​
Too little silver​
      Acetate group calcined off​
      Silver couldn't be doped in easily​

## Slide 36: Next Steps
  PXRD (Powdered X-ray diffraction)
    to analyze chemical structure
  XIA α-particle counter tests in progress
  Future procedure must adjust to match commercial results​
    Different Ag concentrations and reagents​
    Different O2 scavenging methods​

## Slide 37: Selective precipitate has promising results for lowering background

## Slide 38: Acknowledgements
Steve Maguire
Nasim Fatemighomi
Scientific Support Team
Peter Qin
Connor Stubbs
Martin Blanco

## Slide 39: Thank You for Listening

## Slide 40: Extra Slides

## Slide 41: WHO IS LUCAS??
Henry F. Lucas
May 3, 1926 — Nov 12, 2020
September 1957
Improved Low-Level Alpha-Scintillation Counter for Radon https://pubs.aip.org/aip/rsi/article-abstract/28/9/680/299355/Improved-Low-Level-Alpha-Scintillation-Counter-for?redirectedFrom=fulltext
"he focused his research on the health effects of Radon Gas and went on to invent the Lucas Cell, which is recognized as a sensitive, reliable method for measuring Radon"
https://www.trimblefuneralhomes.com/obituaries/henry-f-lucas

## Slide 42: Experiment - Selective Precipitate
  Wet solid
  Baked at 40-45C
  46g: ~97% yield
https://www.sciencing.com/chemical-reactions-involved-baking-cake-7173041/