## Slide 1: Cracking the Crate: Tracking the SNO+ Suspects with X-Rays
Julia Gorovitz
Supervisors: Christine Kraus, Matt Depatie, Mark Ward, Ryan Bayes, Stefan Kaluzienski
CASST 2026
1

## Slide 2: Contents
Introduction
Copper Creep Corrosion
XRF Spectroscopy Analysis
Data Findings and Discussion
Conclusion and Future Directions
Acknowledgements
2
Notes: Outline it better

## Slide 3: Introduction 01
The SNO+ Experiment
3

## Slide 4
SNO+:
9000+ PMTs
  Infrastructure inherited from SNO
Acrylic vessel
  780 tonnes of LAB
Surrounded by 7 kt of UPW, with a 2 km rock overburden
4
Diagram credits: https://snoplus.phy.queensu.ca/about.html
Notes: Point out age of electroncs, don’t talk about nickel mine stop getting distracted

## Slide 5
HV Cables connected to PMT Interface Cards
5
Diagram credits: Andy Mastbaum (2014)
Notes: Lead soldering, circuits made of copper

## Slide 6
electronics
Well said, Uncle Ben!
What challenges come with so much (old) hardware to maintain?
6

## Slide 7: Copper Creep Corrosion 02
“Dark matter”
7
Notes: Mention dark matter joke

## Slide 8: What is it?
Mine air contains H2S and moisture
Circuit boards made of copper -> oxidation!
2Cu + H2S + ½ O2 → Cu2S + H2O
8
Photo credits: https://knowledge.ni.com/KnowledgeArticleDetails?id=kA00Z000000kIpsSAE
Notes: Maybe talk about mine here instead, don’t talk so much about oxidation here

## Slide 9: In our boards
Photo credits: Oluwasemoore Tijani and Mark Ward
Causes short circuits and creates unwanted connections because of the copper sulfide
How do we quantify it?
9
Notes: Mention lead, really really point out this problem

## Slide 10: X-Ray Fluorescence 03
Using spectroscopy to find the culprit
10

## Slide 11: Methods
Tapelifts are taken
Tapelifts pick up corroded copper
12
Diagram reference: https://www.horiba.com/int/scientific/technologies/energy-dispersive-x-ray-fluorescence-ed-xrf/xrf-key-components/
Notes: Focus more!!! Don’t be boring

## Slide 12: The theory
Non-destructive technique based on X-Ray emissions of electrons “jumping down”
11
Diagram reference: https://ywcmatsci.yale.edu/gallery/xrf/principle
Notes: https://www.technologynetworks.com/analysis/articles/x-ray-fluorescence-xrf-theory-practice-and-applications-396212

## Slide 13: Data processing
Fe and Ca standards
  Used to calibrate the energy
13
Notes: Be concise here please, just say the energy hets calibration

## Slide 14: Data processing
Calibration: Fe and Ca
  Known standards are used to correct the spectra
Blank subtraction
  Remove backgrounds from the machine/ tapelifts
14
Notes: Molybdenum xrf source if anyone asks :D correct the blank part

## Slide 15: Daughterboard example
Kα
Kβ
Very tiny Pb Lα
15
Notes: Ask mark about the lead vs copper

## Slide 16: Data Findings & Discussion 04
16

## Slide 17: Element distributions by crate
17
Counts
Slot
Crate
Notes: Redo this one compressing the separate days into one same crate, be moreobjective!!!!! Say that its fairly coherent

## Slide 18: Correlation between elements
Rank difference
18
Notes: *investigate zinc more*mPandas, don’t spend too much time explaing this!! Just say it’s a correlation matrix and we’re good, nickel was used in smal amounts for corrosion prevention (in case someone asks)

## Slide 19: Conclusions and Future Directions 05
Ideas for the next detectives on the case
19

## Slide 20: Conclusions
Several recurring Cu and Pb hotspots were identified
Cu, Ni, and Zn frequently rank high at the same locations
Large variations between crates! Additional measurements are needed before identifying a definitive corrosion pattern, but, the FEC’s were already cleaned :(
20

## Slide 21: Future Directions
More tapelifts per location for improved statistical accuracy
Conclude tapelifting the remaining crates
Re-do tapelifts in newly clean FECs
Tapelift with time: week after, month after, semester after, etc… to keep track of the culprit’s action
Compare elements statistics to failure statistics
21

## Slide 22: Special Thanks!
Dr. Christine Kraus, Juliette Deloye, Dr. Nasim Fatemi-Ghomi, Dr. Lorna Nolan, Dr. Mark Ward, Matt Depatie, Dr. Ryan Bayes, Stefan Kaluzienski

## Slide 23
Goals of the experiment:
Neutrinoless double beta decay (0νββ)
Solar neutrinos
Geo antineutrinos
Reactor antineutrinos

## Slide 24
This is a real front-end card!
In SNO+ we have 300+ of these, each with four daughterboards
Distributed in 19 crates in the deck:
Notes: Picture of a rack!

## Slide 25: Element distributions by crate
20

## Slide 26: Element distributions by crate
19

## Slide 27: Data processing
Calibration: Fe and Ca
  Known standards are used to “correct” the spectra
Calibration: Fe and Ca
  Known standards are used to “c
Blank subtraction
  Remove backgrounds from the machine/ tapelifts
Argon normalization
  Correct for inflation in peaks from more and more radiation
15